| Institution: Faculty of Chemistry and Chemical Engineering Department of Science and Engineering Oxide Materials and Nanomaterials Laboratory of design, obtaining and characterization ceramics Address: 11 Arany Janos Str, room 14 Tel: 0264 593833 Contact person: Assoc prof. Dr. Ing. Gorea Maria e-mail: mgorea@chem.ubbcluj.ro |  |
| --- | --- |
| Equipment: ToniPERM Electronic Permeability Tester |
| Characteristics and performances: The apparatus is suitable for determination of the mass-related specific surface of dispersed solid according to the permeation techique (Blaine method) in the range between approx. 1000 la 4000 cm2/g. Volume of the gauge head – approx 74 cm3; Electric connection – voltage: 230 V ± 10 %; frequency: 50 sau 60 Hz; power: 15 VA; Date of purchasing: 2007 |
| Applications: Determination of the specific surface (Blaine value) of powders; Data are evaluated entirely automatically; The Blaine value is calculated as the average of the individual values; The measurement process serves as a practice-oriented alternative to standard procedures according; Rapid test setup; Once the test is set up, the apparatus can automatically carry out as many Permeation measurements as required. |
| Offer addressed to potential internal and external users: The experimental facilities will be available correlated to the schedule of the teaching program performed in the laboratory Costs will be agreed according to the custom’s particular experimenting program |
| Funding source: Funds for the development of didactic laboratories |
| Estimated value: 46755 RON |